| PHYSICAL SPECIFICATION |
| --- |
| Nominal Voltage Nominal Capacity (10HR) | 12V 60Ah |  |
| Dimension | Length Width Container Height Total Height | 258±2mm （10.16 inches） 133±2mm (5.24 inches) 200±2mm (7.87 inches) 200±2mm (7.87 inches) |  |
| Weight | Approx. 18.1 Kg ( 39.89lbs) |  |
| Standard Terminal | Bolt-and-nut terminal Bolt Type: M5 |  |
| ELECTRICAL SPECIFICATION |
| Characteristics | Discharge curves @ 25℃ (77 °F) |
| Capacity | 10 hour rate (6A) 5 hour rate (10.2A) 3 hour rate (15A) 1hour rate (36A) | 60Ah 51Ah 45Ah 36Ah |  |
| Capacity affected by temperature | 40℃ （104 0F） 25℃ （77 0F） 0℃ （32 0F） | 102% 100% 85% |  |
| Internal Resistance | Full charged battery (25℃,77 0F) 6mΩ |  |
| Designed life | ≥720 Cycles @ 50% DOD (25℃) |  |
| Constant Voltage Charge | Cycle | Initial Charging Current less than 15A Voltage 14.1~14.4V at 25℃ (77 0F ) Temperature Coefficient –5mV/℃ |  |
|  | Standby | No limit on Initial Charging Current Voltage 13.5~13.8V at 25℃ (77 0F ) Temperature Coefficient –3.3mV/℃ |  |